**MAGNET RECEPTIVE**

**UV-PRINTABLE WALLCOVERING**

**54” WIDE WITH NON-WOVEN BACKING**

**SPECIFICATIONS**

## Total Weight 20.50 oz / Sq Yd

Top Layer 4 mil Printable PET Smooth

Base Layer 8 mil Iron Oxide

Backing 4 mil Cellulose Non-Woven

## Total Thickness 16 mil

## Width 54”

## Roll Length 50 feet

## 

## Flame Resistance Class A (ASTM E-84)

Flame Spread 10, Smoke Developed 25