**EXHIBIT ONE PROJECTION DRY ERASE COATING - TEST RESULTS**

**TEST ASTM METHOD RESULT**

VOC D3960 < 100 g/l

Density D1475 9.44 lbs / Gal

Sag Resistance D4400 < 3 mils

Crack Resistance/

Elongation D522 > 32%

Gloss 60 degree D523 50 or less @ 3 mil coating

QUV/500 Hrs, D4587 Visual Gloss Change - Minimal

UVA 340 Visual Color Change – NONE

Other Detrimental Film Effects-NONE

DE = 1.40

Flammability E-84 Flame Spread – 5

Smoke Development – 0

Flashpoint D92 > 140 F

Scrub Resistance D2486 > 15,000 Cycles

Washability D3450 98.8%