**EXHIBIT ONE PROJECTION DRY ERASE COATING - TEST RESULTS**

 **TEST ASTM METHOD RESULT**

 VOC D3960 < 100 g/l

 Density D1475 9.44 lbs / Gal

 Sag Resistance D4400 < 3 mils

 Crack Resistance/

 Elongation D522 > 32%

 Gloss 60 degree D523 50 or less @ 3 mil coating

 QUV/500 Hrs, D4587 Visual Gloss Change - Minimal

 UVA 340 Visual Color Change – NONE

 Other Detrimental Film Effects-NONE

 DE = 1.40

 Flammability E-84 Flame Spread – 5

 Smoke Development – 0

 Flashpoint D92 > 140 F

 Scrub Resistance D2486 > 15,000 Cycles

 Washability D3450 98.8%