**STANDARD DRY ERASE WALLCOVERING**

**SPECIFICATIONS (Gloss and Low Glare)**

Total Weight 14.75 oz / sq yd

Composition PVC (11.65 oz / sq yd)

Backing 50% Polyester / 50% Cotton

(3.15 oz / sq yd)

Total Thickness 15 mils

Width 60”

Flame Resistance Class A (ASTM E-84)

Solvent Resistance 1000 Double rubs w/ MEK

(ASTM D 4752)

Colorfastness Class 4.5 – 5 at 200 AFU

(AATCC 16E)

Abrasion Resistance 20,000 Double Rubs / Wyzenbeek

(ASTM D 3597)