**48” MAGNET RECEPTIVE DRY ERASE**

**WALLCOVERING WITH NON-WOVEN BACKING**

**(Gloss and Low Glare)**

**SPECIFICATIONS**

## Total Weight 47.25 oz / Sq Yd

Composition PET (18.30 oz / sq yd)

Backing 100% Cellulose (1.25 oz / Sq Yd)

## Total Thickness 27 mils

## Width 48”

##

## Flame Resistance Class A (ASTM E-84)

## Solvent Resistance 1000 Double rubs w/ MEK

## (ASTM D 4752)

## Colorfastness Class 4.5 – 5 at 200 AFU

## (AATCC 16E)

## Abrasion Resistance 20,000 Double Rubs - Wyzenbeek

## (ASTM D 3597)

##